TECHNICAL    DATA   SHEET:

Epoxy Base Zinc Rich Grey Primer

Type: Two Pack Air Drying Type.

Composition:Epoxy Resin(with 60%Zinc ) & Polyamide Cured.

Mixing Ratio: Base : Hardner---3:1

Thinner Addittion: 15-20% of mixed paint.

Shelf Life: 12 mths.

Pot Life: 4—5Hrs

Application: Conventional Spray or Airless Spray only.

Uses: On  M.S. Fabricated Jobs, Structures, Railings,Furniture,etc. for mild chemical resistance,etc. It can be overcoated with Epoxy,Polyurethane Topcoats.

Sr.No.           Properties                                Specifications

1)                    Colour                                Grey

2)           Appearance                             Matt & Smooth

3)           Specific Gravity                     1.45---1.55Kg/L.

4)           Viscosity                        95---105Secs in Ford CupB4(at 30to35D.C.)

5)         Covering Capacity                  85—95Sq.Ft./L. per coat

6)         D.F.T.                                     50—60 microns per coat

7)        Drying Time:

a) Touch Dry                              35--60 mins.

b) Surface Dry                            2Hrs---4Hrs

c) Hard Dry                               20—24Hrs.

8)      Overcoat Interval                        20—24Hrs.

9)     Scratch Hardness                        Up to 3 Kg.wt.

10)   Flexibility                                   No cracking of film at 180 degrees.

11)   Thinner Recommended              EpoxyThinner

12)   Resistance Properties                 Water, Humidity,Mild Acids &

Alkalys, etc.

Directions For Use: The surface to be painted has to be  properly free of Rust,Grease,Water,etc.The Epoxy Base Zn. Rich Grey Primer has to be mixed thoroughly and then mixed with Epoxy Hardner in 3:1 ratio. 10%--15% Epoxy Thinner  has to be mixed with the mixture and stirred properly before spraying.

After painting the job has to be kept for airdrying in a dry, dust free environment.

Painted jobs are to be tested only after 72Hrs. Airdry.

Precautions:1)The painting has to be done at a uniform air pressure of 25-35lbs.

2) The containers are to be kept airtight after use.

3) The epoxy primer has to be mixed thoroughly before each use.

4) Application should be done in open dry weather, but avoid windy climate.

5) Use mask while painting.