TECHNICAL    DATA   SHEET:

Epoxy Base Coal Tar

Type: Two Pack Air Drying Type.

Composition:Epoxy Resin & Polyamide Cured.

Mixing Ratio: Base : Hardner---4:1

Thinner Addittion: 25-30% of mixed paint.

Shelf Life: 6 mths.

Pot Life: 4—5Hrs

Application: Conventional Spray or Airless Spray only.

Uses: On  M.S. Fabricated Jobs, Structures, Railings,Furniture,etc. for mild chemical resistance,etc.It is used as an excellent protective coat for water tanks,mild chemical tanks,storage tanks,water proofing medium,etc.

Sr.No.           Properties                                Specifications

1)                    Colour                            Reddish Black

2)           Appearance                             Semi-Glossy & Smooth

3)           Specific Gravity                     1.25---1.3Kg/L.

4)           Viscosity                              120—130 secs in Ford CupB4.

5)         Covering Capacity                  55—65Sq.Ft./L. per coat

6)         D.F.T.                                     50—75 microns per coat

7)        Drying Time:

a) Touch Dry                              3--4 Hrs.

b) Surface Dry                            8---10Hrs

c) Hard Dry                               12—16Hrs.

8)      Overcoat Interval                        16—20Hrs.

9)     Scratch Hardness                        Up to 3 Kg.wt.

10)   Flexibility                                   No cracking of film at 180 degrees.

11)   Thinner Recommended              EpoxyThinner

12)   Resistance Properties                 Water, Humidity,Mild Acids &

Alkalys,etc.

Directions For Use: The surface to be painted has to be  properly free of rust,grease,water,etc.The Epoxy Base Coal Tar has to be mixed thoroughly and then mixed with hardner in 4:1 ratio. 25%--30% Epoxy Thinner  has to be mixed with the mixture and stirred properly before spraying.

After painting the job has to be kept for airdrying in a dry, dust free environment.

Painted jobs are to be tested only after 72Hrs. Airdry.

Precautions:1)The painting has to be done at a uniform air pressure of 25-35lbs.

2) The containers are to be kept airtight after use.

3) The Coal Tar Epoxy has to be mixed thoroughly before each use.

4) Application should be done in open dry weather,but avoid windy climate.

5) Use mask while painting.