RISHABH RESINS & CHEMICALS

(AN ISO 9001:2008 CERTIFIED COMPANY)

Office & Factory: Plot No.15 E & F, Sri Venkateshwara Co-op. Industrial Estate,

IDA Jeedimetla, Hyderabad – 500 055, Telangana, India.

Ph: +91-40-40213105, 23096104, ( Fax: +91-40-23097040

Email: rrc@rishabhgroup.com, nilesh@rishabhgroup.com, Web: www.rishabhgroup.com

CARDANOL (CASHEW PHENOL)

INTRODUCTION:

Cardanol is abstracted and purified from natural Cashew Shell oil (CNSL). It is a natural renewable and excellent raw material to produce Phenolic resin and Epoxy hardener because it can replace or partially replace Phenol.

Cardanol is also applied in epoxy resins and substitute many Phenols to synthesize new materials such as Surfactants, High performance Phenolic resins etc., due to its unique molecular structure.  Cardanol has the reactivity as the oil with Phenol as it is a kind of single hydroxyl phenol which has long hydrocarbon chain that contains hydrogen. When compared with Petroleum/Synthetic Phenol, Cardanol has high performance and are very environmental-friendly due to its lower price.

APPLICATIONS:

Cardanol is widely used in the following fields:
1. Liquid or pulverous thermoset Phenolic resin: improve the flexibility and water resistance of

common Phenolic resin, high-performance laminated board.
2. Epoxy resin hardener, Epoxy resin ameliorant;

3. Liquid phenol: Epoxy resin adhesive, Epoxy resin anti-corrosion coating;

4. Cardanol friction material such as Brake Shoe pads & Clutch facings. 
5. Substitute Tung oil (China wood oil) widely applied in fields of coatings, Copper clad

Laminates (CCL), Paper-based Laminates, Printing inks, etc.
6. Light-colored Cardanol is suitable for surface coating & Paints.
7. Foundry resins

8. Insulating Varnishes.

# TECHNICAL SPECIFICATIONS OF CARDANOL

### PROPERTIES                                              SPECIFICATIONS

## Colour          				          Pale Amber Colour

On Gardener Scale                                       Between 6-8

## Appearance				          Transparent Liquid

Specific Gravity @ 30°C (cps)			0.920 – 0.940

Viscosity @ 30°C (cps)       			45.0 – 60.0

Acid Value                          			Max 5

Iodine Value (wij’s method)            		Between 230 – 250

Hydroxyl value                              		Between 180 – 200

Ph Value                                                         Between 4-6

Moisture Content                                          0.1% Max

Ash Content                                                   Nil