RISHABH RESINS & CHEMICALS

(AN ISO 9001:2008 CERTIFIED COMPANY)

Office & Factory: Plot No.15 E & F, Sri Venkateshwara Co-op. Industrial Estate,

IDA Jeedimetla, Hyderabad – 500 055, Telangana State, India.

Ph: (O) +91-40-40213105, 23096104, (H/P) +91 9391023105

Email: rishabhresins@gmail.com, nilesh@rishabhgroup.com, Web: www.rishabhgroup.com

# Technical Write-Up of Silex-50 Pure CNSL Phenolic Resin

Introduction: Silex-50 is a Pure Cashew Nut Shell Liquid based Phenolic Resin and is processed using special catalyst to cater to the need of various dark coloured but quick drying paints and primers. The resins has got both air drying and baking properties and is suitable for making High Gloss Dark & Semi Dark colored Enamels & Paints, Anti Corrosive Primers, Red Oxide Metal Primers, Anti Fouling Paints, Insulating Varnishes, Anti Termite Chemicals and Varnishes, Black offset Printing Inks of outstanding properties particularly in regard to resistance to the water and chemical.

Compatibility: Silex-50 is compatible with all Drying oils, Alkyds, Epoxies, Ester gums, Phenolics, Maleics etc., in all proportion and only to a limited extent in Chlorinated Resins specially Chlorinated Rubber. It is not compatible with Urea resins.

Solubility: Silex-50 is soluble in Mineral Turpentine oil (MTO) in all proportion. It is also soluble in most of the common paints solvent like Toluene, Xylene, Naphtha’s, Ester etc., but having limited solubility in Epoxies, Vinyl & Ethyl Ketones.

Recommended Driers: Driers such as 1% lead or 0.5% cobalt and 1.5% Manganese as metal on the solid resin content is recommended. If require the proportion of Manganese can be increased to further 1.0% with beneficial effects. After addition of driers ageing for 24 hours is recommended.

Mode of Supply: It is supplied in 200 kg’s packing’s as 100%, 80%, and 70% solids. For most of the paints and varnishes applications 70% execution is recommended as it has the best film properties & flowable from drums.

Specifications:

| Solid | Consistency | Colour | Specific Gravity | Viscosity @ 50% sol’n in Seconds in B4 Ford Cup | Drying time | Scratch Hardness Air Dried | Acid Value |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | Surface Dry | Hard Dry | At 1200C |  |  |
| 100% | Highly Viscous Non Pourable | Dark Reddish Brown | 0.92 + 0.02 | 50 to 80 | 30-45 mts | 3-4 hrs. | ½ hour | 1000 | Max 5 |
| 80% | Highly Viscous Pourable | Dark Reddish Brown | 0.92 + 0.02 | 60 to 100 | 30-45 mts | 2-3 hrs | ½ hour | 1000 | Max 5 |
| 70% | Semi Viscous Free flowing | Dark Reddish Brown | 0.92 + 0.02 | 100 to150 | 30-45 mts | 2-3 hrs | ½ hour | 1100 | Max 5 |

Cont’d...2

RISHABH RESINS & CHEMICALS

(AN ISO 9001:2008 CERTIFIED COMPANY)

Office & Factory: Plot No.15 E & F, Sri Venkateshwara Co-op. Industrial Estate,

IDA Jeedimetla, Hyderabad – 500 055, Telangana State, India.

Ph: (O) +91-40-40213105, 23096104, (H/P) +91 9391023105

Email: rishabhresins@gmail.com, nilesh@rishabhgroup.com, Web: www.rishabhgroup.com

::2::

Comparative Film Properties: The film properties of Silex-50 at 30% solid in MTO with Linseed oil Ester gum Varnishes and 66% Oil length Alkyd varnishes are as follows:

| Film Properties | Silex - 50 (70%) Resins | 66% oil length Alkyd Resins | Linseed Oil Ester gum Resins |
| --- | --- | --- | --- |
| Colour | Golden Reddish | Pale | Light yellow |
| Hard-dry time | 3 to 4 hours | 4 to 5 hours | 5 to 6 hours |
| Appearance | Highly glossy | Glossy | Glossy |
| Scratch Hardness | 1100 gm’s | 600 gm’s | 1000 gm’s |
| Adhesion | Good | Good | Good |
| Flexibility | Good | Better | Good |
| Resistance to water | NE (100) | SB (8) | SB (25) |
| Sodium Carbonate 5% | NE (100) | SB (25) | FB (25) |
| Sulphuric Acid 2% | NE (100) | SB (48) | FB (50) |
| White Spirit | NE (100) | NE (100) | NE (100) |
| 25% Linseed Oil | NE (100) | SB (100) | SB (25) |

Note:   NE- No Effect                   SB- Slight blushing

FB- Film blushed 	           SE- Slight effect

Figures in Bracket indicates No. of Hours

Application Technique: Film of Silex-50 can be applied either by Brush, Spray or Dipping technique.

Storage: The storage stability is Silex-50 is satisfactory for 6 months or more if stored in air tight containers in a cool place.

Recommended uses: Silex-50 either alone or in combination with other resins and used for formulating Primers, Dark & Semi Dark coloured Enamels and Paints, Insulating Varnishes, Knifing Putty, Black offset Printing inks and similar other applications including special purpose Anti Corrosive Paints & Primers, Anti Fouling Paints, Baking composition etc.

Caution: Some times Silex-50 may be used along with basic pigment like Zinc Chrome,

Zinc Oxide, Basic Lead Sulphates etc. It is advised that these pigments are not ground along

with the main pigment in the CNSL resin as there is a possibility of reaction. The reactive

pigments should be added after the grinding for proper dispersion of the Pigment. Hence it

is advisable to grind the main pigments with any Long Oil Alkyd Resin and then add our

CNSL resin outside and stir well to avoid reaction.

……………………..X………………………