rishabh RESINS & cHEMICALS

hyderabad, india

(AN ISO 9001-2008 CERTIFED COMPANY)

SILEX 50 (70%) PLAIN CNSL PHENOLIC RESIN

Technical Data Sheet

Chemical / Physical nature

Silex 50 (70%) is a low viscous, monomer free             Storage guidelines

CNSL based Plain Phenolic resin based on a	         The resin should be stored indoors in the special  original composition. 			         unopened and undamaged packaging, in a dry

place at temperatures between 25°C and 40°C.

Shelf life is reduced at higher temperatures and

the properties of the resin might change during

storage.

Exposure to sunshine should be avoided.

Major applications

Silex 50 (70%) is a pure CNSL based Resin                   Material Safety Data Sheet

and is processed using special catalysts to cater        A material safety data sheet for the product is

to the needs of various dark coloured but quick          available on request.

drying paints and Industrial Primer. The resin has

got both air drying and baking properties and is

suitable for making high gloss enamels, dark

coloured paints, primers and varnishes of

outstanding properties particularly in regard to the

resistance to water and chemicals.

The resin has excellent storage stability.

Test methods

Test methods (TM) referred to in the table(s) are

available on request.

Product specifications upon delivery

| Properties | Test Result |
| --- | --- |
| Appearance | Reddish Yellow Viscous Resin |
| Solid Content | 70+/-2% |
| Specific Gravity @ 30°C | 0.90 – 0.92 |
| Viscosity @ 30°C @ 50% in Mineral Sprit /MTO with B4 Ford Cup | 120 – 150 seconds |
| Acid Value (mgmKOH/gm) | Max 5 |
| Scratch Hardness | 1100 gms |
| Resistance to Water & Chemicals | Excellent |
| Drying Time (With Combination Driers) | Surface Dry: 45 Min’s Hard Dry: 3 Hours Tack Free: 20 Hours |

Factory & Office:

Plot No.15 E & F, Sri Venkateshwara Co-op Industrial Estate

Jeedimetla, Hyderabad – 500 055, Telangana, INDIA

Ph: +91-40-23096104, 40213105

Email: rrc@rishabhgroup.com ; rishabhresins@gmail.com

Web: www.rishabhgroup.com