rishabh RESINS & cHEMICALS

hyderabad, india

SILAC U 210 (SINGLE PACK PU RESIN)

Technical Data Sheet

Chemical / Physical nature

Silac U210 is a low viscous, monomer free                                 Storage guidelines

Urethane Oil based Alkyd resin based on a special                  The resin should be stored indoors in the original, composition. They are Polymers built up by               unopened and undamaged packaging, in

Urethane linkages containing air dry Polyunsaturated             a dry place at temperatures between 25°C

ester groups as substitutes. In effect the modern Urethane     and 30°C.

Oils are a type of Alkyd Resin in which the Di-basic acid is     Shelf life is reduced at higher temperatures

Replaced by a Diisocyanate.                                                        and the  properties of the resin might

These Resins are very rapid drying. Flexible film but film        change during storage.

Yellows slightly with time.                                                            Exposure to sunshine should be avoided.

Major applications                                                                          Material Safety

Silac U210 are widely used in a very wide range of                    A material safety data sheet for the product is applications. Some of the areas where they have shown      Available on request

considerable promises are:

Water Proofing of Cement Structure,

Furniture Finishes, Fast Dry super Enamels,

Leather Industry, Rubber & FRP Industry,

Chemical Process Industry, Wooden Bobbins etc.

Test methods

Test methods (TM) referred to in the table(s) are

available on request.

Product specifications upon delivery:

| Properties | Test Result |
| --- | --- |
| Appearance | Yellow Light Pale Transparent Liquid |
| Solid Content | 60+/-2% |
| Specific Gravity @ 30°C | 0.90 – 0.92 |
| Viscosity @ 30°C @ 50% in Mineral Sprit /MTO with B4 Ford Cup | 80 - 100 seconds |
| Acid Value (mgmKOH/gm) | < 4 |
| Free NCO | < 0.01% |
| Scratch Hardness | ≥ 1500 gms |
| Colour | Max’m 4 on Gardener |
| Solubility | Infinite soluble in Mineral Spirits/ Toluene and other solvents |
| Oil Type | Linseed |

Although the facts and suggestions in this publication are based on our own research and are believed reliable, we cannot assume any responsibility for performance or results obtained through the use of our products herein described, nor do we accept any liability for loss or damages directly or indirectly caused by our products. The user is held to check the quality, safety and all other properties of our product prior to use. Nothing herein is to be taken as permission, inducement or recommendation to practice any patented invention without a license.

Factory & Office:

Plot No.15 E & F, Sri Venkateshwara Co-op Industrial Estate

Jeedimetla, Hyderabad – 500 055, Telangana, INDIA

Ph: +91 40 23096104, 40213105 ( Fax: +91-40-23097040

Email: rrc@rishabhgroup.com ; nilesh@rishabhgroup.com Web: www.rishabhgroup.com

GREEN INDIA ****** CLEAN INDIA