### S  F  C

Gala No - 423, 4Th Floor Gundecha Industrial Complex Premises

Co-Op Soc.Ltd,Mumbai -400101, PHONE : 0091-22-28845476- 28844891,

E-Mail: alokgoenka_in@yahoo.com /karandmevada@gmail.com

# Website: www.shreejifinechem.com

## TECHNICAL SPECIFICATION OF

ZINC CHLORIDE ANHYDROUS

POWDER

| PARTICULARS | VALUE |
| --- | --- |
| ZnCL2 | 98.5 |
| NH4CL | 1.4 |
| Pb ppm | 0.3 |
| Cd ppm | 0.3 |
| Fe ppm | 1.6 |
| Mn ppm | 0.2 |
| SO4 ppm | 71 |
| Basic salt (Zno) | 1.23 |