S  F  C

# Gala No 423, 4th Floor Gundecha Industrial Estate Premises CO-OP ltd,

# Akurli Road, Kandivali (E) Mumbai: 4000101.

TEL # 28845476/ 28844891

E-Mail: alokgoenka_in@yahoo.com / karandmevada@gmail.com

# Website: www.shreejifinechem.net

### CERTIFICATE OF ANALYSIS

ZINC CARBONATE

###### IMPORTED

| PARTICULARS | VALUE |
| --- | --- |
| ZN (%) | 58.2 |
| Pb (ppm) | 0.5 |
| Cd (ppm) | 0.3 |
| Fe (ppm) | 5.2 |
| Mn (ppm) | 1.0 |
| Cu (ppm) | 0.2 |
| H2O (%) | 1.6 |
| Average particle 325 mesh | 99.99% pass |
| packing | 25kg |