S  F  C

# Gala No 423, 4th Floor Gundecha Industrial Estate Premises CO-OP ltd,

# Akurli Road, Kandivali (E) Mumbai: 4000101.

TEL # 28845476/ 28844891

E-Mail: alokgoenka_in@yahoo.com /karandmevada@gmail.com

# Website: www.shreejifinechem.net

TECHNICAL SPECIFICATION OF

CALCIUM CHLORIDE

70%- 75%PURITY

| PARTICULARS | GRADE |
| --- | --- |
| PURITY | 70%-75% |
| PHYSICAL APPERENCE | WHITE SMALL LUMPS |
| WHITENESS | MILKY WHITE |
| MATTER INSOLUBLE IN WATER (% BY Wt.) MAX. | 0.40 |
| Mg Cl2 (% By Mass) MAX | 0.7 |
| NaCl (% By Mass) MAX | 1.6 |
| MAGNESIUM & ALKALI SALT AS SULPHATES (% By Mass) MAX | --- |
| Ph (5% soln 25°c) MAX | 8.0 |
| HEAVY METALS as Pb (% By Mass) MAX | 0.005 |
| Fe (% By Mass) MAX | 0.001 |
| SOLUBILITY (10% Soln) | CLEAR |
| ALKALINE CHL | 0.30 |
| PACKING | 50KG.BAG |