S  F  C

# Gala No 423, 4th Floor Gundecha Industrial Estate Premises CO-OP ltd,

# Akurli Road, Kandivali (E) Mumbai: 4000101.

TEL # 28845476/ 28844891

E-Mail: alokgoenka_in@yahoo.com / karandmevada@gmail.com

# Website: www.shreejifinechem.net

CERTIFICATE OF ANALYSIS

### STEARIC ACID 921

| S.NO | PARAMETER | SPECIFICATION | UNITS | METHOD | RESULTS |
| --- | --- | --- | --- | --- | --- |
| 1 | Description | White flakes, a clear transparent liquid on melting. Free from adulterants and foreign matter |  |  | Complies |
| 2 | Acid Value | 198.0 Min | mgKOH/g | IS:548-1964 | 208.40 |
| 3 | Iodine Value | 3.0 Max | g 12/100g | IS:548-1964 | 0.45 |
| 4 | Color (Lovibond in 5 ¼” Cell) | 3.0Y+1.0R Max | Units | IS:548-1964 | 1.0Y+0.1R |
| 5 | Titer | 54-62 | Deg C | IS:548-1964 | 55.6 |
| 6 | SaponificationValue | 199.0 Min | mgKOH/g | IS:548-1964 | 208.96 |
| 7 | Ash Content by mass | 0.10 Max | % | IS:1675-1971 | 0.054 |