S  F  C

# Gala No 423, 4th Floor Gundecha Industrial Estate Premises CO-OP ltd,

# Akurli Road, Kandivali (E) Mumbai: 4000101.

TEL # 28845476/ 28844891

E-Mail: alokgoenka_in@yahoo.com / karandmevada@gmail.com

# Website: www.shreejifinechem.net

TECHNICAL SPECIFICATION OF

STEARIC ACID 911

| PARTICULERS | VALUE |
| --- | --- |
| APPEARANCE | WHITE FLAKE |
| MELTING POINT TITRE0C | 0.55 |
| ACID NUMBER | 213.16 |
| SAPONIFCATION | 214.06 |
| IODINE NUMBER | 0.5 |
| COLOUR LOVIBOND 51/4 CELL | 0.8Y+0.1R=1.3 |
| ASH CONTENT | 0.088 |