**YASH MINERALS (MINES OWNER &SUPPLIERS OF INDUSTRIAL MINERALS) EMAIL; -** [**mineralsroyal@gmail.com**](mailto:mineralsroyal@gmail.com)**,** [**yashmierals13@gmail.com**](mailto:yashmierals13@gmail.com)

**CHINA CLAY POWDER**

**Dear sir,**

**We are the professional manufacturer of mining minerals and we have specialized in CHINA CLAY AND CALCITE POWDER,DOLOMITE POWDER from many years. We are supplying our product to as a regular basis for use in their production process . our factory located at JAITARAN and UDAIPUR we want to give you best rate and the best quality CHINA CLAY & DOLOMITE powder AND CALCITE POWDER**

**Analysis report**

**Sr.no. particulars specification according to mesh**

**250 300 400 500**

1. **sio2 45.84% 42.39% 38.11% 35.36%**
2. **cao 1.38% 1.37% 01.365%**
3. **mgo 0.38% 0.25% 0.20% 00.715%**
4. **fe2o3 0.50% 0.36% 00.690%**
5. **al2o3 30.39% 36.88% 33.90% 35.845%**
6. **loi 12.43% 12.39% 12.485%**
7. **na2o 0.20% 0.12% 00.295%**
8. **k2o 1.14% 0.15% 00.655%**
9. **tio2 0.32% 0.30% 0.05%**
10. **ph value 8.30% 7.90% 8.55%**
11. **whiteness 80% 81.39% 82.89% 85.05%**
12. **acid soluble 2.25% 2.30% 2.20% 2.365%**
13. **oil absourtion 20.88 21.88% 20.02% 44.850%**
14. **water absourtion 32.00 34.00% 38.46% 31.730%**
15. **moisture 0.29 0.25% 0.22% 0.05%**
16. **Bulk density 00.675% 00.585% 00.498% 00.485%**

**YASH MINERALS**