S  F  C

# Gala No 423, 4th Floor Gundecha Industrial Estate Premises CO-OP ltd,

# Akurli Road, Kandivali (E) Mumbai: 4000101.

TEL # 28845476/ 28844891

E-Mail: alokgoenka_in@yahoo.com / karandmevada@gmail.com

# Website: www.shreejifinechem.net

CERTIFICATE OF ANALYSIS

ZINC CHLORIDE TECHNICAL

| PARTICULARS | VALUE |
| --- | --- |
| Property | Technical powder |
| Purity | 81.54 % |
| Zinc Content | 38.50 % |
| Appearance | Snow-white |
| Ammonia as NH 4 Cl | 8-10% |
| Alkalies and Alk.Earth | 2% |
| Iron and Lead | 0.005% |
| Dry Basis Assay | ----------- |
| Packing | 25 Kg |